## Slide 1: Nanotechnology principles and instrumentation
October 7th, 2025
Cancer Engineering Foundations
Lecturer: Christian Figueroa-Espada, Ph.D.

## Slide 2: Outline
Nanotechnology, why should you care?
Definitions
Instrumentation
Physical concepts
Some potentially disruptive (nano)technologies

## Slide 3: What is the definition of a nanoparticle/nanomaterial?
A nanoparticle/nanomaterial must have at least one dimension with a size of:
a.) 1 – 10 nm
b.) 1 – 100 nm
c.) 10 – 1000 nm
d.) 1 – 1000 nm

## Slide 4: Nano: why should you care?

## Slide 5: Nano: why should you care?
Proteins, what are they?
Proteins are nanoparticles
IgG Antibody
Laminin-1
Helen G. Hansma. Varieties of imaging wih scanning probe microscopes PNAS 1999 96 (26) 14678-14680; doi:10.1073/pnas.96.26.14678
Atomic Force Microscopy

## Slide 6: Biomacromolecules are nanoscale
DNA is a nanoribbon

## Slide 7: Nanoscale is bio-scale

## Slide 8: Nanotechnologies for medicine and biomedical research
Drug delivery
Into live cells and tissues
For research and therapy
Targeted delivery
New therapeutic mechanisms
Imaging and Detection
Molecular imaging
Contrast agents
Sensor technologies
Research Tools
Quantification (sensors)
Imaging (probes)
Macromolecule delivery
Lipofectamine
pH Sensitive NPs
http://web.mit.edu/biomaterials/Irvine_Lab/research/Entries/
2011/9/5_nanoparticles_for_intracellular_drug_and_vaccine_delivery.html
Kong F, Zhou F, Ge L, Liu X, Wang Y - Int J Nanomedicine (2012)

## Slide 9: Nanotechnology: measurement techniques
How to measure/characterize nano-sized materials?
Techniques include:
Transmission electron microscopy
Scanning electron microscopy
Atomic force microscopy
Dynamic light scattering
Zeta potential measurement

## Slide 10: Transmission electron microscopy
Electron beam is transmitted through an ultra-thin specimen.
Specimen absorbs electrons to create contrast.
Resolution down to 0.5 Ångströms (50 pm)
Notes: Simple idea: TEM uses a beam of electrons (instead of light) that passes through a very thin sample to form an image.
How it works:
Electrons travel through the sample.
Dense areas block more electrons and appear darker.
The detector or screen captures how electrons are transmitted to form a highly detailed image.
What it tells you:
The internal structure of materials at the atomic or nanometer scale.
You can see crystal lattices, defects, nanoparticles, or organelles inside cells.
Analogy: Like shining a flashlight through a leaf and seeing the veins — but at a million times higher resolution.

## Slide 11: Scanning electron microscopy
Avian Flu Virus
Culicoides biting midge
Platinum “Nanothorns”
Electron beam hits sample, creating secondary electrons emitted by atoms in the sample.
Specimen should be electrically conductive or can be coated with an ultra-thin layer of gold.
Resolution down to 1 nanometer
Apoptotic HeLa Cell
Notes: Simple idea: SEM scans the surface of a sample with electrons and detects signals coming off the surface.
How it works:
A focused electron beam “scans” over the surface.
The way electrons bounce back (secondary or backscattered electrons) depends on surface shape and composition.
Detectors collect these signals to form a detailed 3D-like image.
What it tells you:
The surface morphology and texture of a sample.
Useful for nanostructures, coatings, biological samples, or materials with rough surfaces.
Analogy: Like using your fingertip to “feel” the surface, but using electrons to “see” it in incredible detail.

## Slide 12: Atomic force microscopy
Principle:
Cantilever with a nano-sized tip is dragged over a surface.
Laser reflection off of cantilever records changes in height.
Resolution down to 0.1 nm
(in z direction)
Images surface topology
Measures binding affinity
Measures elastic modulus
Imaging possible in native conditions
(in buffers/on live cells)
Notes: Simple idea: AFM uses a tiny, sharp tip that feels the surface of a sample — like a record player needle tracing grooves — but at the atomic scale.
How it works:
A sharp probe scans across the sample surface.
As it moves up and down due to surface features, a laser beam measures those deflections.
This data is turned into a height map — an image of the surface topography.
What it tells you:
The surface structure down to atomic resolution.
Also gives information about mechanical, electrical, or chemical properties.
Analogy: Like blindfolded touch — “feeling” atoms instead of seeing them.

## Slide 13: Atomic force microscopy
Budhathoki-Uprety, et. al., JACS, 2014
Polymer-Encapsulated Carbon Nanotubes
Gold nanoparticles on a silk film

## Slide 14: Atomic force microscopy
(a) Ion-driven rotors from spinach chloroplast and (b) Illyobacter tartaricus FoF1-ATP synthase26, 27. (c) High-light-adapted native photosynthetic membrane from Rhodospirillum photometricum16. (d) Perfringolysin O pore complexes14. (e) Dimeric bovine rhodopsin (dotted ellipse) in native disc membranes28. (f) Extracellular surface of gap junction hemichannels29. Contact mode AFM topographs were recorded in buffer solution at forces of 100 pN or less
Amyloid Fibrils
F1-ATPase
Membrane Proteins
Science 5 August 2011: vol. 333 no. 6043 755-758
Knowles, Cambridge University

## Slide 15: Atomic force microscopy can measure force and live cell mechanics
Science 5 August 2011: vol. 333 no. 6043 755-758
Knowles, Cambridge University
Samples:
Nanomaterials
Single biomolecules
Live cells
Force measurements

## Slide 16: Atomic force microscopy equipment @ Tri-I
Asylum Instruments Bio AFM 3D
MSKCC Molecular Cytology Core Facility
Zuckerman C4 Basement

## Slide 17: Dynamic light scattering
Measures:
Particle size: ~0.3 nm – 8 µm
Molecular weight: ~1x103 – 2x107 Da
Zeta potential: (particle surface charge)
Principle:
Particles in solution scatter light. This light
then undergoes either constructive or destructive interference by the surrounding particles. By this intensity fluctuation, information is contained about the time scale of movement of the scatterers.
Data produced:
Autocorrelation function, which is then fitted to equations to give particle size
Notes: Simple idea: DLS measures how light scatters off particles in a liquid to determine their size.
How it works:
A laser shines through a suspension.
Tiny particles move randomly (Brownian motion), causing scattered light to fluctuate.
The rate of these fluctuations tells you how fast the particles move — and from that, their hydrodynamic size.
What it tells you:
The average particle size and size distribution in a liquid (e.g., nanoparticles, proteins, micelles).
Analogy: Imagine watching dust motes dancing in sunlight — DLS mathematically measures how fast they “dance.”

## Slide 18: Dynamic light scattering
DLS measures the Hydrodynamic Radius
of the Particle
Stokes radius, Stokes-Einstein radius, aka hydrodynamic radius RH, is the radius of a hard sphere that diffuses at the same rate as the molecule.
Autocorrelation function data
of particles with different sizes

## Slide 19: Zeta potential
Zeta potential (ζ-potential) is a measure of electrostatic potential on the surface of a particle (colloid). It is thought of as the overall charge of a particle. It can help predict the long-term stability of a particle in solution.
More precisely, zeta potential is the electric potential at the slipping plane—the plane that separates mobile fluid from fluid that is attached to the particle.
Zeta potential of a particle can be positive or negative, just as the overall charge of the nanoparticle can be positive or negative. The larger the absolute magnitude, the better the stability of the particle.
Notes: Simple idea: Zeta potential tells you about the surface charge of particles in a liquid — which affects how stable a suspension is.
How it works:
An electric field is applied to the sample.
Charged particles move (electrophoresis), and their velocity is measured using light scattering.
The movement relates to the zeta potential — a measure of electrostatic repulsion.
What it tells you:
Whether particles are likely to clump together or stay dispersed.
Important for colloidal stability, formulation, and nanoparticle research.
Analogy: If each particle is like a magnet — zeta potential tells you how strongly they repel or attract each other.

## Slide 20
If you want to image a nanoparticle inside of a cell, which technique(s) could you use?
Transmission Electron Microscopy
Scanning Electron Microscopy
Atomic Force Microscopy
Dynamic Light Scattering
Zeta Potential Measurement

## Slide 21: Nanotechnologies: some physical concepts and potentially useful materials
PAPER DISCUSSION

## Slide 22: Nanotechnology – what is unique?
Quantum size effect: electronic properties of certain solids are altered with great reductions in particle size.
Quantum dots: Emission wavelength is size-dependent

## Slide 23: Quantum dots
Emission wavelength is size-dependent
Highly Photostable

## Slide 24: Quantum dots are versatile nanoprobes
Can be linked to proteins, etc.
Commercially available:

## Slide 25: FRET: Förster resonance energy transfer
(Sometimes: Fluorescence resonance energy transfer)
To measure the distance between molecules (up to 10 nm)

## Slide 26: FRET: measures distance between molecules
Distance is calculated from the
FRET ratio
aka. Relative FRET efficiency

## Slide 27: FRET: measures distance intramolecularly too
https://micro.magnet.fsu.edu/primer/techniques/fluorescence/fret/fretintro.html

## Slide 28: FRET: measures distance intramolecularly too

## Slide 29: Plasmonics: silver and gold
Surface Plasmon Resonance: the collective oscillation of valence electrons in a solid stimulated by incident light
-Causes greatly increased electric fields near metals such as gold and silver
Surface Plasmon Resonance (Biacore) is a label-free surface assay which use changes in the index of refraction on a gold surface to detect the binding of proteins and other molecules.
Localized Surface Plasmon Resonance:
SPR on a nanoparticle

## Slide 30: Surface-enhanced Raman scattering (SERS)
Raman scattering near gold or silver (film or particles) is greatly enhanced. Can be used for imaging or sensing
Paxon, et. al. 18 April 2011, SPIE Newsroom. DOI: 10.1117/2.1201103.003645

## Slide 31: Raman scattering
Paxon, et. al. 18 April 2011, SPIE Newsroom. DOI: 10.1117/2.1201103.003645
adenine
cytosine
guanine
thymine
uracil
Selection rules
Based on symmetry elements of polarizability tensor
Vibrational fingerprint
Comprised of narrow spectral features
Robust mechanism
Not subject to photobleaching
Weak Signal
Compared to Rayleigh scattering / fluorescence
Provides rich info. about structural data!

## Slide 32: SERS enhancement
Chemical Enhancement
Based on metal-molecule charge-transfer effects
Electromagnetic enhancement
Coupled to surface plasmon excitation of metal nanostructures
Plasmon resonance leads to local field enhancement near the surface
Adsorbed molecules see increased field
Raman signal enhancement (up to 1015)
Depends on local geometry of adsorption site
Away from plasmon resonance
At plasmon resonance

## Slide 33: Raman scattering: applications
S.M. Nie, et al., Science, 275 1102 (1997)
http://www.oxonica.com/diagnostics/diagnostics_sers_imaging_applications.php
Molecular fingerprinting
Unique vibrational spectra distinguishes molecules
Tagless biosensing
Fluorescent dyes are not needed
Multiplexed sensing
Plasmon resonances allow for sensor tunability
In vivo applicability
Near-IR excitation and biocompatability
Femtomolar and beyond
Single molecule spectroscopy is possible
1500 cm-1
1532cm-1
1600cm-1
1635cm-1

## Slide 34
Some More
Potentially Disruptive (Nano)Technologies

## Slide 35
Microlithography, Nanolithography, and Micro/Nanoprinting
Photolithography
E-beam Lithography

## Slide 36
Lithography for Single-Cell Analysis
A high-throughput single-cell analysis of human CD8+ T cell functions reveals discordance for cytokine secretion and cytolysis
Varadarajan, et. al. J Clin Invest. 2011;121(11):4322–4331. doi:10.1172/JCI58653.
Useful for measuring differences among populations, screening of phenotypes

## Slide 37
Microcontact Printing
Neurons migrate to patterned peptide
Patterned IKVAV peptide
Heller, et. al. Biomaterials (2005) 26, 883-889.

## Slide 38
Microfluidic Devices: Lab on a Chip
Use nanoliters of fluid for many applications:
Assays/microarrays
Control of cell environment
Single cell measurements
Drug screening

## Slide 39
Microfluidic Device Application: Single-Cell Microarray
Shi, et. al. PNAS, 2011

## Slide 40: Thank you! 